## Slide 1
ME-11102 – Work shop
Dr.R PRABHU SEKAR,
Assistant Professor,
Mechanical Engineering Department,
Motilal Nehru National Institute of Technology Allahabad.

## Slide 2: Course Topic -2
2. Materials in Design –Evolution of Engineering materials –Metals-
Plastics -composites Applications – Automotive Industry-
Consumer Goods- Construction & Civil Structure- Industrial
Applications.

## Slide 3: Evolution of Engineering Materials
Materials play an important role for our day to day needs ,and even for our survival.
In the stone age the naturally accessible materials were stone, wood, bone, etc..
Gold was the 1st metal used by the mankind followed by copper.
In the bronze age Copper and its alloy like bronze was used and in the iron age they discovered Iron (pig iron).
zz
Click to add text

## Slide 5: Evolution of Engineering Materials

## Slide 6: Why Material Engineering Important to Technologists?
Mechanical engineers search for high temp material so that gas turbines, jet engines etc., can operate more efficiently and wear resistance materials to manufacture bearing materials
Electrical engineers search for materials by which electrical devices or machines can be operated at a faster rate with minimum power losses
Aerospace & automobile engineers search for materials having high strength-to weight ratio
Electronic engineers search for material that are useful in the fabrication & miniaturization of electronic devices
Chemical engineers search for highly corrosion-resistant materials
Note: All these demands may be fulfilled when the internal structure and engineering properties are known to an engineer or technologist

## Slide 7: The Evolution of Materials in Products
In this section we consider one example of the changes in the way materials are used, each spanning about 100 years.
The kettle is the oldest of household appliances and the one found in more homes than any other.
1. Kettles
Cast Iron
Bronze
Polypropylene

## Slide 8: The Evolution of Materials in Products
Early kettles, heated directly over a fire, were of necessity made of materials that could conduct heat well and withstand exposure to an open flame: iron, copper, or bronze .
Electric kettles, developed in the 1890s, had external heating elements to replace the flame, but were otherwise much like their predecessors.
All that changed with the introduction, by the Swan company (1922), of a heating element sealed in a metal tube placed within the water chamber.
The kettle body no longer had to conduct heat—indeed for safety and ease of use it was much better made of a thermal and electrical insulator.
Today almost all kettles are made of plastic, allowing economic manufacture with great freedom of form and color.

## Slide 9: The Evolution of Materials in Products
2. Aircraft
Early planes were made of low-density woods (spruce, balsa, and ply), steel wire,5 and silk. Wood remained the principal structural material of airframes well into the twentieth century, but as planes got larger it became less and less practical.
The aluminum airframe, exemplified by the Douglas DC3, was the answer. It provided the high bending stiffness and strength at low weight necessary for scale-up and extended range.
Aluminum remained the dominant structural material of civil airliners for the remainder of the twentieth century.

## Slide 10: The Evolution of Materials in Products
By the end of the century, the pressure for greater fuel economy and lower carbon emissions had reached a level that made composites an increasingly attractive choice, despite their higher cost and greater technical challenge.
The future of airframes is exemplified by Boeing’s 787 Dreamliner (80% carbon-fiber–reinforced plastic by volume), claimed to be 30% lighter per seat than competing aircraft.
All this has happened within one lifetime.
Competitive design requires the innovative use of new materials and the clever exploitation of their special properties, both engineering and aesthetic.

## Slide 11: Classification of Engineering Materials
It is the systematic arrangement or division of materials into groups on the basis of some
common characteristic
1. According to General Properties
2. According to Nature of Materials
3. According to Applications

## Slide 12: Classification of Engineering Materials
According to General Properties
(a). Metals (e.g. iron, aluminium, copper, zinc, lead, etc.) Iron as the base metal, and range from plain carbon (> 98 % Fe)
(i). Ferrous: high alloy steel (< 50 % alloying elements), e.g. cast iron, wrought iron, steel, alloys like high-speed steel, spring steel, etc
(ii). Non-Ferrous: Rest of the all other metals and their alloys, e.g. copper, aluminium, zinc lead, alloys like brass, bronze, duralumin, etc.
(b). Non-Metals (e.g. leather, rubber, asbestos, plastics, etc)

## Slide 13: Classification of Engineering Materials
2. According to Nature of materials
Metals: e.g. Iron & Steel, Alloys & Super alloys, Intermetallic Compounds, etc
(b) Ceramics: e.g. Structural Ceramics (high-temperature load bearing), Refractories (corrosion-resistant, insulating), White wares (porcelains), Glass, Electrical Ceramics (capacitors, insulators, transducers), Chemically Bonded Ceramics (cement & concrete)
(c) Polymers: e.g. Plastics, Liquid Crystals, Adhesives.
(d) Electronic Materials: e.g. Silicon, Germanium, Photonic materials (solid-state lasers, LEDs)

## Slide 14: Classification of Engineering Materials
(e) Composites: e.g. Particulate composites (small particles embedded in a different material), Laminate composites (golf club shafts, tennis rackets), Fiber reinforced composites
(fiberglass).
(f) Biomaterials: e.g. Man-made proteins (artificial bacterium), Biosensors, etc.
(g) Advanced / Smart Materials: e.g. materials in computers (VCRs, CD Players, etc), fibreoptic systems, space crafts, aircrafts, rockets, shape-memory alloys, piezoelectric ceramics, magneto strictive materials, optical fibres, micro electromechanical (MEMs) devices, electro-rheological / magneto-rheological fluids, Nano-materials, etc.

## Slide 15: Classification of Engineering Materials
3. According to Applications
(a) Electrical Materials: e.g. conductors, insulators, dielectrics, etc.
(b) Electronic Materials: e.g. conductors, semi-conductors, etc.
(c) Magnetic Materials: e.g. ferromagnetic, paramagnetic & diamagnetic materials, etc.
(d) Optical Materials: e.g. glass, quartz, etc.
(e) Bio Materials: e.g. man-made proteins, artificial bacterium

## Slide 17: Classification of Engineering Materials

## Slide 18: Materials Properties
Physical: e.g. appearance, shape, weight, boiling point, melting point, freezing point, density, glass transition temperature, permeability.
2. Mechanical: e.g. strength (tensile, compressive, shear, torsion,
bending), elasticity, plasticity, ductility, malleability, rigidity,
toughness, hardness, brittleness, impact, fatigue, creep, strain
hardening, vibration, wear.
3. Thermal: e.g. thermal conductivity, expansion coefficient,
resistivity, thermal shock resistance, thermal diffusivity

## Slide 19: Materials Properties
4. Electrical: e.g. conductivity, resistivity, dielectric strength.
5. Magnetic: e.g. Ferromagnetism, Paramagnetism,
magnetic permeability, curie temperature.
6.Chemical: e.g. reactivity, corrosion resistance, polymerization,
composition, acidity.
7. Optical: e.g. reflectivity, refractivity, absorptivity, transparency,
opaqueness, color,

## Slide 20: Young’s Modulus
Hook’s law: With in the elastic limit, the stress is very nearly proportional to the strain. The nominal tensile strain, for example, is proportional to the tensile stress; for simple tension

## Slide 21: Young’s Modulus
Diamond is at the top, with a modulus of 1000GPa. Soft rubbers and foamed polymers are at the bottom with moduli as low as 0.001GPa.
Most ceramics and metals have moduli in a comparatively narrow range: 30–300GPa. Cement and concrete (45GPa) are near the bottom of that range. Aluminum (69GPa) is higher up; and steels (200GPa) are near the top.
Polymers are quite different: all of them have moduli which are smaller.

## Slide 22: Young’s Modulus of composites
Is it possible to make polymers stiffer?
The answer is yes—if we mix into the polymer a second, stiffer, material. Good examples of materials stiffened in this way are:
GFRP - Glass-fiber reinforced polymers, where the polymer is
stiffened or reinforced by long fibers of soda glass;
(b) CFRP - Carbon-fiber reinforced polymers, where the reinforcement
is achieved with fibers of graphite;
(c) KFRP -Kevlar-fiber reinforced polymers, using Kevlar fibers
(a unique polymer with a high density of covalent bonds
oriented along the fiber axis) as stiffening;
(d) Filled polymers - polymers into which glass powder or silica flour
has been mixed to stiffen them;

## Slide 23
5. Material Selection – Civil structure
The Wooden Bridge (1749)
Cast Iron arches (1823)
Stone Bridge (1640)
Mild steel bridge (1950)

## Slide 24
In the eighteenth century the ready availability of cast iron, with its relatively low assembly costs, led to many cast-iron bridges.
Metallurgical developments of the later nineteenth century allowed large mild-steel structures to be built.
Finally, the advent of cheap reinforced concrete led to graceful and durable structures This evolution clearly illustrates how availability influences the choice of materials.
5. Material Selection – Civil structure
Reinforced concrete bridge
150 years or so ago wood was commonly used for bridge building. It was cheap, and high-quality timber was still available in large sections from natural forests.
Stone, too, was widely used.

## Slide 25
Ferrous Alloys
Steels:
Iron it its purest form is not used as an engineering material because it has poor tensile strength and hardness. But when alloyed with other elements, the properties can be greatly improved or modified.
Out of the various alloying element, carbon is the most important element.
The maximum amount of carbon that can be alloyed with iron is 6.67% (the maximum solubility of carbon in iron).
Carbon content upto 2% in iron is termed as steel and above 2% are called as cast iron.
Steels have other than carbon, small amount of elements such as manganese, sulphur, phosphorous and silicon.

## Slide 26
Ferrous Alloys
The properties of steel are influenced by an increase in carbon content which has the following effects:
Tensile strength is increased
Greater hardness is obtained
Ductility is decreased
Weld ability – (the ability of a material to be weld) is decreased
Toughness is improved

## Slide 27
Classification of steels on the base of carbon
Steels may broadly be classified as
Carbon steels (plain carbon steels)
Alloy steels
Carbon steels
These are known as plain carbon steel or simply steel.
The percentage of carbon in most steels range from 0.1% to 2%.
Carbon steels are classified as
Low carbon steel (Mild steel) : 0.008 to 0.3% Carbon
Medium carbon steel : 0.3 to 0.6% Carbon
High carbon steel : 0.6 to 2% Carbon

## Slide 28
1. Low carbon steels
This is also known as soft steel. It is used where ductility and softness are important and high tensile strength is not required.
The hardness of plain carbon steel increases with carbon content.
It is important to note that the percentage of carbon in low carbon steel is upto 0.3% and this amount of carbon is not sufficient for steel to undergo the heat treatment process.
So the hardness of low carbon steel cannot be increased by conventional heat treatment method.
They can be case hardened (the outer surface can be made hard by heating it in an atmosphere of carbon).
The hardness of low carbon steel is only about 150 BHN.

## Slide 29
1. Low carbon steels
Applications:
It is used for manufacturing products such as screws, nails, nut, bolts, washers, wire fences, automobile body sheets.
It is also used in the form of sheets, squares, rounds, plates, and wires.
Steels with 0.15 to 0.3% carbon are used as structural steels and find applications as building bars, grills, beams, angle, channels etc.

## Slide 30
2. Medium carbon steels
The carbon content ranges between 0.3% to 0.6%.
Medium carbon steels have greater tensile strength and hardness than low carbon steels.
The hardness around 300 BHN.
They also have better machining qualities.
They are difficult to cold worked and hence are usually hot worked.
Applications:
1. They are used for making hooks, wire ropes, shafts, connecting rods, spindles, rail axels, gears, turbine bucket, steering arms.

## Slide 31
3. High carbon steels
The carbon content ranges between 0.6% to 2%.
They have higher tensile strength and are harder than other carbon steels. They have hardness about 500 BHN.
High carbon steels responds readily to heat treatment and hence their hardness can be further increased to desired values
.
They have good wear resistance.
The hardenability is more than medium carbon steels.
These steels cannot be cold worked and are hence always hot worked.

## Slide 32
Applications :
1. They are used for making hand tools such as wrenches, chisels, punches and rail wheels, files, cutting tools like drills, wood working tools and rod for reinforced concrete.
3. High carbon steels

## Slide 33
Alloy steels
Alloy steels are those steels which contain other elements like Ni, Mn, W, Cr, Mo, V etc.
These elements are added to plain carbon steel to improve one or more of the following properties:
Greater strength, hardness, toughness at low and high temperatures
High hardenability
Greater wear resistance
Lesser tendency to cracking
More uniform properties throughout the cross section
More resistance to corrosion
Greater flexibility in heat treatment is possible.

## Slide 34
Alloy steels
Alloy steels can be classified as low alloy steels and high alloy steel.
Steel is said to be low alloy steel if the total percentage of alloying elements is less than 8%.
Steels is said to be high alloy steel if the total percentage of alloying elements is more than 8%.
Every alloying element present in steel contribute a certain property to it.

## Slide 35
Influence of alloying elements in steels
Aluminum:
Aluminum is a deoxidizer and restricts grain growth.
When aluminum is added small amount, it increased strength, however too much aluminum causes embrittlement.
Aluminum ranges from 2 to 5 % imparts resistance to heat and oxidation.
Boron
Boron is a very powerful hardening agent, however it is a very expensive element.
Hence, boron is used in small quantity not over 0.003%.
When too much boron is added, it produces brittleness.

## Slide 36
Influence of alloying elements in steels
Chromium:
Chromium forms hard carbides and imparts good wear resistance corrosion resistance and high hardness.
Chromium decreases machinability.
When more than 5% chromium is added, the high temperature properties and corrosion resistance of the steel will be greatly improved.
Copper
Copper is added in steel ranging from 0.1 to 0.4%.
Copper increases resistance to atmospheric corrosion and also strengthens steels.

## Slide 37
Influence of alloying elements in steels
Nickel:
Nickel is mainly used in alloy steels in amounts upto about 5% to increase strength and toughness.
The presence of nickel in large amounts increases resistance to oxidation at high temperature.
Nickel also decreases the machinability
Phosphorus:
Phosphorus is kept below 0.5% in most of the steels.
It increases the tensile strength, hardness and also improves machinability.

## Slide 38
Influence of alloying elements in steels
Tungsten:
Tungsten forms strong carbides and strengthens steels. These carbides provide wear and abrasive resistance to the steel.
It gives red hardness (also called hot hardness, it is the ability of the material to maintain strength at high temperature).
Hence, tungsten is an important element in most high speed tool steels and hot working die steels.

## Slide 39
Cast Iron
By melting Pig iron along with iron scraps and limestone in a cupola furnace Cast iron is obtained.
Cast iron is a ferrous materials, it is basically an alloy of iron and carbon. The cast iron can have any carbon percentage between 2 to 6.67%.
The practical limit is normally between 2 to 4%. Too much carbon makes the iron very brittle.
Although cast iron is brittle and has lower strength properties than most steel it has certain advantages.

## Slide 40
Cast Iron
Advantages of Cast Iron
Cast iron has a lower melting temperature (1140 -1200 C) than steel (1380- 1500 C), hence it can easily be cast.
It possesses high casting property such as high fluidity, low shrinkage and ease of production. It can be cast into any shape.
They have very high compressive strength, about 3 to 4 times that of its tensile strength. The base of heavy machines are usually made of cast iron.
Cast iron can be easily machined (good machinability)
They provide high wear resistance.
Because of high carbon content, they have self lubricating properties hence lathe machine bed are made of cast iron.
Cast iron has high damping capacity.

## Slide 41
Types of Cast Iron
White cast iron :
It is called white cast iron because it shows a white surface when it broken.
The carbon percentage ranges from 2 to 3.6%. It is very hard and brittle. The hardness varies from 350 to 500 BHN.
White cast iron is obtained by making the molten metal to cool and solidify rapidly. On solidification iron carbide gives a white colour to the cast iron.
It has high compressive strength so it is very difficult to machine white cast iron.
Applications
It has good wear resistance and is used for making rolls for rolling mills, grinding balls, wearing plates.

## Slide 42
Types of Cast Iron
2. Grey cast iron :
It is called white cast iron because it shows a grey surface when it broken.
The carbon percentage ranges from 2.4 to 3.8%. It is very hard and brittle. The hardness varies from 150 to 320 BHN.
Grey cast iron is obtained by allowing the molten metal to cool and solidify slowly. On solidification graphite flakes gives a grey colour to the cast iron.
It has good machinability and it has low melting point.
It has good shock resistance.
Applications
1. Grey cast iron is used for making machine bed, tables, IC engine cylinder block, cylinder head, flywheels, electric motor body, car wheel drum.

## Slide 43
Types of Cast Iron
3. Chilled cast iron :
Chilled cast iron is a combination of both white and grey cast iron. In this, the molten metal is solidified in a chiller mold.
The surface which gets rapidly cooled becomes white cat iron and the inner which gets slowly cooled becomes grey cast iron.
Chilled cast iron is made by careful cooling and maintaining a proper cooling rate.
Applications
1. Chilled cast iron is used for making Forging dies, sprockets, cam shaft, grinding balls.

## Slide 44
Types of Cast Iron
4. Malleable cast iron:
As the name suggests, malleable cast iron has the ability to be deformed and bendable.
Malleable cast iron is obtained by prolonged heat treating white cast iron at high temperature (950 -970 c), this results in the formation of rounded nodules of graphite.
Malleable cast iron has 2.5% carbon and 1% silicon.
It is less brittle and hence stronger and tougher.
It readily absorbs shock load and vibrations.
It has good machinability and high resistance to corrosion.
It has hardness in the range of 140 – 285 BHN.
Applications
1. It is used for making spanners, lever, sewing machine and hand wheels.

## Slide 45
Non-ferrous alloys
Major non-ferrous alloys
Copper and its alloys
Aluminium and its alloys
Nickel and its alloys
Zinc and its alloys
Lead and its alloys
Tin and its alloys
Bearing metals

## Slide 46
Important Properties of non-ferrous alloys
High resistance to corrosion
Ease of fabrication to any shape by casting, rolling and forging
High electrical conductivity
Very good thermal condutivity
Light weight
Softness and cold workability
Non-ferrous alloys
Click to add text

## Slide 47
Copper and its alloys
Copper is extracted from its ore, called copper pyrites. Pure copper has the following properties
High electrical and thermal conductivity
Good corrosion resistance
Better machinability
Good ductility
It is non magnetic and has a pleasing reddish colour.
1. Arsenical copper : Arsenic, when added upto 0.3%, improves corrosion resistance of copper.
This is used in condensers, heat exchangers.
2. Free cutting copper: Tellurium, when added to 0.6% improves machinability of copper.
This is used for making bolts, studs, electrical parts such as switch gear, relays, contact pins.

## Slide 48
Copper and its alloys
3. Silver bearing copper : Silver, when added upto 0.1% prevents softening of copper during soldering process.
4. Phosphorised copper: Phosphorous, when added upto 0.02% controls the electrical conductivity of copper
I. Brasses: Brass is an alloy of copper and zinc.
Addition of zinc in varying percentage results in improving color, strength, machinability, hardness of the alloy.
70% copper and 30% Zn is called as α-brass . It shows higher ductility and corrosion resistance.
Gilding Metal (95% Cu and 5% Zn): It shows good ductility and better pressing ability. It is used medals, coins, tokens, jewelry.
Red Brass (85% Cu and 15% Zn): This alloys show improved corrosion resistance. It is used for condenser and heat exchanger tubes.

## Slide 49
Copper and its alloys
Munz Metal (60% Cu and 40% Zn): It is most widely used brass. It is used in pump parts as valve, condenser tubes, brazing rods and utensils.
Brazing Brass (50% Cu and 50% Zn): It is used for joining of brasses.
Cast Brass (85%Cu, Tin 5%, Lead 5% and Zinc 5%): This brass shows a good castability and machining property. It is also called as leaded gun metal (or) ounce metal. It is used in low pressure valves, pipe fittings, and small pump casting.
II. Bronzes:
If any alloy of copper contains any alloying elements other than zinc, it is called as bronze. In general, copper and tin alloy called as bronze.
Gun Metal (88% Cu, 10% tin and 2% zinc): It is used for making gun barrels and other ordinance components.

## Slide 50
Copper and its alloys
Phosphor Bronze (10% tin, 0.03 to 0.25 % phosphorus and balance copper): It shows excellent casting properties. It is used for making bearings and bushes due to antifriction properties.
Leaded bronze (or) Plastic bronze: It contains lead in the range of 5 to 24%, tin around 2% and balance copper. It shows the highest bearing properties and is used for bearing applications.
.
Copper – Nickel alloys
Cupronickel : Ni 30% and Cu 70%. It has a higher resistance to corrosion, fatigue resistance. It is used for condensers, heat exchanger tubes.
Constantan : Ni 45% and Cu 55%. This alloy has a very high electrical resistivity. Constantan is used in the form of wires for making resistors and thermocouples.

## Slide 51
Nickel Silvers :
These are the alloys of copper, nickel and zinc.
A typical composition contains 50 to 70 % Cu, 5 to 30 % Ni, 4 to 30% Zn.
The addition of nickel to copper zinc alloy gives it a silver blue white colour.
They are also called as German Silver.
They show a higher corrosion resistance and better cold working properties.
Silver and chromium can be effectively plated on these alloys.
They are used for rivets, screws, jewelry.
Copper and its alloys

## Slide 52
Aluminium and its alloys
Aluminium :
It is one of the most used non-ferrous metal. It is alloyed with silicon, copper, and magnesium to improve its properties.
Some of the important properties of aluminium are as follows,
It is light in weight. It has low density which is almost one third that of iron.
It has low melting point (660 c)
It shows better corrosion resistance
It shows higher ductility and malleability
It has good heat and electrical conductivity
It has a good machinability
It is non magnetic and non-sparking

## Slide 53
Aluminium and its alloys
Duralumin: 4% Cu and rest Al. It shows good hardness and strength. It is used in aircraft industry.
LM 5 – 5% Mg and balance Al. Good weld ability and corrosion resistance. It is used in cable.
LM 10 - 10% Mg and balance Al. It is used for making aircraft and automobile parts.

## Slide 54
Nickel and its alloys
Nickel shows good corrosion resistance.
Nickel is used mainly for production of stainless steel.
It is also used for electroplating.
Dura Nickel: It is a nickel aluminium alloy. It contains 93.9% Ni, 0.15% C, 0.25% Mn, 0.55% Si and 4.5% Al and Fe, S, Cu and Ti. It shows high corrosion resistance and strength. It is used for bellows, fish hook and parts of fishing equipment.
Monel : It is a nickel copper alloy. It contains 66% Ni, 30% Cu with Fe and Mn. It is used in aircraft instruments.
Electrical resistance alloys: 80% Ni, 20% Cr. Used as heating elements for domestic ovens and industrial furnaces.

## Slide 55
Nickel and its alloys
Inconel: It contains 76% Ni, 16% Cr and 8% Fe.It has good corrosion resistance, strength and toughness. It is used in heaters, dairy equipments.
Invar : It is Nickel – iron alloy with 35% nickel. It does not show any changes in dimensions with a change in temperature. It is used for measuring instruments like gauges, scales, vernier.
Elinvar : It contains 36% Ni, 12% Cr with rest of Iron. It is used in watches for making springs.
Alnico : It contains 8 to 10% Al, 15 to 30% Ni, 5 to 30% Co with Fe. It has high magnetic property. It is used to make powerful magnets. It finds applications in motors, microphones and speakers.

## Slide 56
Lead and tin alloys
Tinman’s solder: It contains 62% tin. It is used for soldering elctronic components.
Plumber’s solder: It contains 20 to 40 % tin. The pasty nature of alloy helps the plumber to join pipes therefore it is called as plumber’s solder.
Terne metal : It contains 10 to 25% tin. It is used for coating steel sheets in order to improve its corrosion resistance.

## Slide 57
Ceramics
Ceramics can be defined as solid compounds that are formed by the application of heat, and sometimes heat and pressure, comprising at least two elements provided one of them is a non-metal or a nonmetallic elemental solid (NMES).
The other element(s) may be a metal(s) or another nonmetallic elemental solid(s).

## Slide 58
Ceramics
Examples:
Magnesia or MgO, is a ceramic since it is a solid compound of a metal bonded to the nonmetal O2.
Silica is also a ceramic since it combines an NMES and a nonmetal.
Similarly TiC and ZrB2 are ceramics since they combine metals (Ti, Zr) and the NMES (C, B)-
SiC is also a ceramic.

## Slide 59
Ceramics
Silicate based ceramics - Pottery, sculpture, sanitary ware, tiles, electrically insulating silicate-based ceramics.
Traditional ceramics are characterized by mostly silicate-based porous microstructures that are quite coarse, non-uniform, and multiphase.
They are typically formed by mixing clays and feldspars, followed by forming either by casting or on a potter's wheel, firing in a flame kiln to sinter them, and finally glazing.

## Slide 60
As a class, ceramics are hard, wear-resistant, brittle, prone to thermal shock, refractory, electrically and thermally insulative, transparent. nonmagnetic, chemically stable, and oxidation-resistant.
As with all generalizations, there will be exceptions; some ceramics are electrically and thermally quite conductive.
Characteristics of Ceramics

## Slide 61
Applications
Insulation- High-temperature furnace linings for insulation (oxide fibers such as SiO2, A12O3, and ZrO2).
Conductivity - Heating elements for furnaces (SiC, ZrO2, MoSi2)
Insulators in electronic applications - Substrates for electronic packaging and electrical insulators in general (Al2O3)
Semiconducting- Thermistors and heating elements (oxides of Fe, Co, Mn).
Gas-sensitive conduct - Gas sensors (ZnO).
Soft magnets - Transformer cores [(Zn)Fe2O3, with Mn, Co, Mg]; magnetic tapes.
Applications of Ceramics

## Slide 62
7. Transparency - Windows (soda-lime glasses), cables for optical communication (ultra-pure silica).
8. Anticorrosion- Heat exchangers (SiC), chemical equipment in corrosive environments
9. Biocompatibility- Artificial joint prostheses (Al2O3)
10. Hardness- Cutting tools (SiC whisker-reinforced A12O3, Si3N4)
11. Wear resistance - Bearings (Si3N4)
Applications of Ceramics

## Slide 63
Plastics
Plastics used for industrial work come from petrochemicals.
Plastic refers to its ability to deform without breaking.
The polymer used in making a plastics are usually a combination of additives, colorants, plasticizers, stabilizers, fillers, and reinforcements.
These additives affect the chemical composition, properties, and mechanical properties of plastics and affect its cost.

## Slide 64
Plastics
The two types of plastics are Thermoplastics and thermosetting polymers.
Thermoplastics
Thermoplastics can be remolded over and over again after heating. Some of these polymers are amorphous and some carry a partially crystalline structure.
Thermosetting Polymers
Thermosetting polymers are those polymers that solidify into a permanent shape. These polymers too are amorphous and have infinite molecular weight.

## Slide 65
Physical properties Plastics
Properties of plastics vary depending on the chemical composition, arrangements and the processing method of its subunits.
Plastics come from polymers, hence all plastics are polymers, but not all polymers are plastic.
Plastics may be amorphous solids or crystalline solids.
They are poor conductors of heat and electricity.
The plastics that act as insulators mostly have a high dielectric strength.
Plastics have a slow rate of degradation and tend to be durable.

## Slide 66
Telephone instruments, plastic toys, ballpoint pens, plastic bowls are thermoplastics and so can be recycled.
Cooker handles carry bags, plastic covering on an electric wire, plastic chains etc are thermosetting plastics and so cannot be recycled.
Physical properties Plastics

## Slide 67
Example of plastics
PEEK - Polyether ether ketone
HDPE – High density polyethylene
EAA - Ethylene-acrylic acid
CN - Cellulose nitrate
EP – Epoxy
PP – Polypropylene
PPG – Polypropylene Glycol
PS – Polystyrene
PUR – Polyurethane
PVC – Polyvinyl Chloride
Plastics

## Slide 68
Because most plastics may be fabricated in the melt and at quite low temperatures (e.g. 200°C) the energy requirements for processing are low. Since plastics generally have low densities, costs of transportation and general handling are also relatively low.
Through the development of such techniques as injection molding it is possible to make highly complex parts in one operation without the need for assembly work or the generation of more than a notional amount of scrap material.
Characteristics of Plastics

## Slide 69
3. Colouring is not usually restricted to the surface but is throughout the mass so that damage due to scratching and abrasion is less obvious than with coated metals.
4. An extremely wide range of surface finishes is possible which may not only simulate non-plastics materials but in addition produce novel effects.
5. The materials are generally excellent thermal insulators, being particularly useful in expanded form.
Characteristics of Plastics

## Slide 70
Characteristics of Plastics
6. Many plastics are superb electrical insulators including, in many instances, good insulation characteristics at high frequencies.
7. Plastics are available in a wide range of strengths, flexibilities and degrees of toughness. Many fibre-reinforced grades have strength per unit weight figures as high as those of many metals.
8. Plastics are available in a wide range of chemical and solvent resistances. Some materials are available that are water soluble whilst others will withstand such aggressive materials as hydrofluoric acid.

## Slide 71
Plastics have been widely accepted as packaging materials.
Plastics bottles have been particularly appreciated in the bathroom, where breakage of glass containers has led to many serious accidents.
The wide use of plastics films for wrapping, for bags
Applications of Plastics

## Slide 72
Applications of Plastics
The automotive industry is now a major user of plastics, with the weight of plastics being used per car increasing year by year.
For many years the main uses were associated with car electrical equipment such as batteries, flex, plugs, switches and distributor caps.
Plastics then became established in light fittings, seating upholstery and interior body trim.
In recent times there has been increased use in under-the-bonnet (under-the-hood) applications such as radiator fans, drain plugs, petrol tubing and coolant water reservoirs.

## Slide 73
Applications of Plastics
Glass-fibre-reinforced plastic boats are widely used as a result of their economy in manufacture, ease of maintenance, lightness of weight and, for military purposes, antimagnetic characteristics.
The non-corrosive nature of plastics also leads to their widespread use in boat fixtures and fittings. In aircraft, plastics are particularly useful on account of their low density.

## Slide 74
Applications of Plastics
Industrial equipment is a continuing area of development for plastics. Pipes, pumps, valves and sight glasses, made from such materials as PVC and poly-4-methylpent-l-ene, have become well established on account of their corrosion resistance.
The nylons are used for such diverse applications as mine conveyor belts and main drive gears for knitting machines and paper-making equipment.

## Slide 75
In the general area of medicine uses range from spare-part surgery, such as hip joints and heart valves, injection syringes.
The photographic industry was of course one of the earliest users of plastics, for photographic film.
use of plastics for tapes, compact discs and toys
Applications of Plastics